## Slide 1
Multi-objective Bayesian optimization for intumescent coating
Eric VERRET, Prof Sophie DUQUESNE, Prof Anthony COLLIN
Univ. Lille, CNRS, INRAE, Centrale Lille, UMR 8207 - UMET - Unité Matériaux et Transformations, F-59000 Lille, France/Université de Lorraine
Pipeline
Wood is more and more used in buildings = sustainable materials compared to concrete and steel
3 Fire tests  4 performance outcome
Horizontal mass loss cone
1 - Total heat released (THR)
2 - Time of ignition (ti)
CFE 1/3 scale
3 - distance of degradation
Determination of distance of degradation via image segmentation (K-means clustering )
Vertical mass loss cone
4 – Median of the mass loss rate
Vertical  more representative of fire in a building and impact gravity on the intumescent char
Conclusion/perspective
References
Intumescent is an efficient method to protect wood against fire in a building
Designs of experiment are very efficient but require high amount of data
The performance of the coating is evaluate by 3 fire tests giving 4 parameters of performance
Multi-objective Bayesian Optimisation has been chosen to find the optimum configuration of the paint (pareto front) and minimize the number of samples
Outlooks
Number evaluation until a satisfactory approximation of the Pareto front is obtained
Comparison between different sampling for initial points
Tonooka, Y., Takaguchi, H., Yasui, K., & Maeda, T. (2014). Life cycle assessment of a domestic natural materials wood house. Energy Procedia, 61, 1634-1637.
Puri, R. G., & Khanna, A. S. (2017). Intumescent coatings: A review on recent progress. Journal of Coatings Technology and Research, 14(1), 1-20.
Weil, E. D. (2011). Fire-protective and flame-retardant coatings-A state-of-the-art review. Journal of fire sciences, 29(3), 259-296.
Naik, D., & Shah, P. (2014). A review on image segmentation clustering algorithms. Int J Comput Sci Inform Technol, 5(3), 3289-93.
Shields, B. J., Stevens, J., Li, J., Parasram, M., Damani, F., Alvarado, J. I. M., ... & Doyle, A. G. (2021). Bayesian reaction optimization as a tool for chemical synthesis. Nature, 590(7844), 89-96.
Wang, Y., Chen, T. Y., & Vlachos, D. G. (2021). NEXTorch: A Design and Bayesian Optimization Toolkit for Chemical Sciences and Engineering. Journal of Chemical Information and Modeling, 61(11), 5312-5319.
Heat flux: 50 KW/m²
Test time: 30 min
Intumescent coating most commune system to protect wood against fire in structures
Aims/objectives
Prediction
Metric | THR | Ti | Median of MLR | Distance of degradation
Mean absolute percentage error (MAPE) | 13% | 17% | 3% | 2%
Coefficient of correlation | 0,67 | 0,73 | 0,89 | 0,67
Fisher exact test p value | 0,011 | 0,011 | 0,0005 | 0,32
The flame propagation is evaluated using a lab-made by small scale
CFE radiant panel test (similar to the ISO5658-2)
Design of Experiement (DoE):
Input
Intumescent coatings react => an expanded structure limiting heat and mass transfer
In Multi-objective optimisation there is typically no single best solution. The Pareto front is the set of solutions where no other solution can improve one objective without sacrificing another. It represents the optimal trade-off between conflicting objectives, providing a range of solutions, to guide decision-making.
Heat flux: 50 KW/m²
Test time: 30 min
Metric evaluation
Error bar: 95% confidence
Model evaluation technique: Leave one out cross-Validation (LOOCV)
Mean of the prediction
95% confidence
Gaussian prior
Output
Input: weight pourcentage
Experimental protocol
Bayesian optimization (BO) is a sequential model-based approach that efficiently explores and exploits the search space to find the optimal solution of a black-box function with limited evaluations. BO can be used for noisy and small dataset.
The coating formulations were obtained a dispersion using a high-speed disperser
A constant dry mass is applied on white fir
The sample is conditioned at 30°C, 40% RH during before the fire testing
Gaussian process fit
High dimension
Multi-objective
Noisy observation